2025年6月6日 SAGA-LS CTR実験log

- Samples

  - #13研削ありCVD 300℃ / TEOS-SiO2

  - #14 研削なしCVD 300℃ / TEOS-SiO2

  - #15 熱酸化膜

Si substrate 250μm thick, TEOS-SiO2/熱酸化膜~200~235nm

- BL15: X-ray energy 8 keV, λ=1.55 Å, PILATUS 100K

HUBER diffractometer

(https://support.spring8.or.jp/BL/bl19b2/huber19/huber.html)

- Si wafer

  - Lattice parameter a=b=c=5.43119

  - Detecting the Si 400 diffraction peak ( θ=34.799,  2θ=69.599,  θ/2θ scan)

- 9:45 #15 熱酸化膜 Stage set

  - Stage height (Sz) adj. / Sample rotation (Ry) adj , etc-> Optimization

  - Detecting the Si 400 diffraction peak ( θ=34.799,  2θ=69.599,  θ/2θ scan) -> optimize

  - Si 400 diffraction peak (θ/2θ scan) θ=34.799±0.5 scanning: -> saved :　Test_02.dat

  - Si_thermo_01.dat:

    - 2θ = 68.592-70.5929, Step 1/100, 1point 10sec accumulation 80 mins -> we found asymmetric diffraction peak at 400

    - Prof. Hirosawa: In the thermos-oxidation, oxygen will insert horizontally, horizontal lattice constant will be expanded, thus the vertical lattice constant will become small 酸化膜だと酸素が水平方向に入って格子が水平面が伸びるので、z方向は縮む->そのような結果に見える。

  - Omega scan: Si_Thermo_01_omega.dat

Beam dump / stopped / 12:00 will be recovered.

  - 12:10 Positioning re-adjust / confirmation:

  - ω-scan under θ/2θ fixed.

- 12:30 Sample change #14 研削なしCVD 300℃ / TEOS-SiO2 ←#15 熱酸化膜

  - Stage height (Sz) adj. / Sample rotation (Ry) adj, etc-> Optimization

  - Detecting the Si 400 diffraction peak ( θ=34.799,  2θ=69.599,  θ/2θ scan) -> optimize

  - Si 400 diffraction peak (θ/2θ scan) θ=34.799±0.5 scanning: -> saved :　TEOS_01.dat

  - Asymmetric feature is opposite to the sample #15. The lattice constant of z direction is considered to be expanded. On the other hand, in the case of #15, the lattice constant of z direction is considered to be compressed.

  - Omega scan: TEOS_01_omega.dat

- 14:20 Sample change #13研削ありCVD 300℃ / TEOS-SiO2←#14 研削なしCVD 300℃ / TEOS-SiO2

  - Stage height (Sz) adj. / Sample rotation (Ry) adj, etc-> Optimization

  - Detecting the Si 400 diffraction peak ( θ=34.799,  2θ=69.599,  θ/2θ scan) -> saved: RoughTEOS_01.dat , RoughTEOS_02.dat

  - Omega scan: RoughTEOS_01_omega.dat

  - 筋はX線入射方向と垂直 / polished stripes are normal direction to incident direction of X-ray

- #13 Sample ϕ 90度回転

  - 筋はX線入射方向と並行 / polished stripes are parallel to incident direction of X-ray

  - Stage height (Sz) adj. / Sample rotation (Ry) adj, etc-> Optimization

  - Detecting the Si 400 diffraction peak ( θ=34.799,  2θ=69.599,  θ/2θ scan) -> saved: RoughTEOS_03.dat , RoughTEOS_04.dat

  - The asymmetric features are almost the same with ϕ=0. This means that the deformation of the z-lattice is common and is independent of the polished stripes.

  - Omega scan: RoughTEOS_02_omega.dat

- 17:20 Sample Change #15 熱酸化膜←#13 Sample 研削ありCVD 300℃ / TEOS-SiO2

  - Purpose: What is the reason for the asymmetric profile on omega-scan data.

  - Sample position is changed. The sample was rotated ~90 degree

  - Detecting the Si 400 diffraction peak ( θ=34.799,  2θ=69.599,  θ/2θ scan)

    - During the scan, the beam intensity / alignment may be fluctuated. -> re-scan

    - It might be the sample moving? (by Prof. Hirosawa) -> sample attachment by manicure is better for holding the sample

    - Method of sample attachments should be considered.

Si_Thermo_02.dat~ Si_Thermo_05.dat

  - Omega scan:

- Sample attachments : M5 60mm□/ total height 36mm / Base plate size 80mm□ /

Center hole on the Base 20phi 20 mm depth

- 電気通信学会学術誌　http://globals.ieice.org/en_transactions/electronics

- PyMC Poisson

  - https://www.pymc.io/projects/docs/en/latest/api/distributions/generated/pymc.Poisson.html

  - https://zenn.dev/inaturam/articles/f2950608a2a2ed

  - https://www.pymc.io/projects/docs/en/stable/api/distributions/generated/pymc.ZeroInflatedPoisson.html